## Slide 1: EASY-CARE FINISH

## Slide 2: INTRODUCTION
Easy-care and durable press finishes are generally applied to cellulose and cellulose blend fabrics, but other fibres can benefit from these finishes also.
The sheen of calendered fabrics (permanent chintz) and the stand and hand of pile fabrics are generally improved by durable press finishes.

## Slide 3: Cont….
The primary effects of the easy-care and durable press finish on cellulosic fibres are reduction in swelling and shrinkage, improved wet and dry wrinkle recovery, smoothness of appearance after drying, and retention of intentional creases and pleats.
The total crease recovery angle (CRA), that is the sum of the crease recovery angles of the warp and the fill directions of the fabric, increases from about 150° to about 300°. A fabric shrinkage of less than 5 % can usually be achieved.

## Slide 4: Cont….
An unavoidable side effect of the cellulosic crosslinking finishes is a reduction in the elasticity and flexibility of the cellulose fibres.
This produces a considerable decrease in abrasion resistance and tear and tensile strengths on natural cellulose fibres.
Easy-care and wrinkle resistance finish is mainly used for woven fabrics.

## Slide 5: Mechanisms of easy-care and durable press finishing
The primary cause of the shrinkage of cellulosic fibres is the fact that these fibres can readily absorb moisture. This absorbed moisture facilitates internal polymer chain movements in the amorphous fibre areas by lubrication. It disrupts the internal hydrogen bonding between these polymer chains.

## Slide 6: Cont….
Two different chemical approaches have been used commercially to produce non-swelling or durable press cellulose fabrics.
The original approach is the incorporation of a polymerized finish in the pores of the fibres, so that water molecules cannot easily penetrate the fibre.
The newer approach is the reaction of multifunctional crosslinking agents with the hydroxyl groups of adjacent cellulose molecules that hinder the swelling of the cellulose fibre.

## Slide 7: Examples of textiles with easy-care and durable press finishes
Easy-care and durable press finishes are applied to cellulose fabrics and fabric blends with high cellulose content that are laundered and which should maintain a smooth, ‘just ironed’ appearance through the lifetime of the article.

## Slide 8: Cont….
Easy-care finishes are also useful in providing dimensional stability to knitted fabrics.
This easy-care finish is also used for table and bed linen because the wrinkling of linen after washing is very marked.
One special use of the cellulose crosslinking finishes are wash permanent chintz articles, produced by the heat and high pressure of calendering the impregnated fabrics.

## Slide 9: Chemistry of easy-care and durable press finishes
Easy-care finishing of cotton has been a major market success since the middle of the 1950s. During the 1960s and 1970s, concern about formaldehyde encouraged development of cellulose crosslinking finishes with low free formaldehyde levels. Continued research has provided products with very low free formaldehyde content as well as products that are completely formaldehyde free.

## Slide 10: Formaldehyde-containing products
TWO DIFFERENT CHEMICAL PROCESS ARE USED—
THE INCORPORATION OF A POLYMERIZED FINISH IN THE PORES OF FIBRE ,SO THAT WATER MOLECULES CAN NOT EASILY PENETRATE THE FIBRE.
THE REACTION OF MULTI FUNCTIONAL CROSS LINKING AGENTS (RESINS) WITH HYDROXYL GROUP OF CELLULOSE MOLECULES THAT HINDER THE SWELLING OF CELLULOSE FIBRES.

## Slide 11: Cont….
RESINS ARE USED AS IT CREATE STRONGER (COVALENT) AND PERMANENT BOND WITH FABRIC THAT REDUCES CREASING TO A LARGER EXTENT.
EXAMPLES ARE----
UREA FORMALDEHYDE RESINS
MELAMINE FORMALDEHYDE RESINS.

## Slide 12: DMU reaction with cellulose

## Slide 13: The main properties of U/F products are
DMU is highly reactive; finish baths have to be used in a few hours
Low stability to hydrolysis, low durability to laundering
High chlorine retention
High content and release of formaldehyde
Very high elastic resilience.

## Slide 14: The main properties of M/F products are:
Better stability to hydrolysis and better washing durability than U/F products
Relatively high formaldehyde content and release
Fewer problems with chlorine retention than U/F products
More dimensional stability and stiffness (also for nylon and polyester).

## Slide 16: Non-formaldehyde containing products
N,N'-Dimethyl- 4,5-dihydroxyethylene urea (DMeDHEU) should not be confused with DMDHEU. DMeDHEU does not contain formaldehyde.

## Slide 18: The main properties of DMeDHEU products are
Formaldehyde free
Very low reactivity
Very low chlorine retention
Limited durability to laundering
Yellowing effect when not ether modified
Price/effect ratio nearly 4:1 compared with DMDHEU
Development of unpleasant odours, depending on the product formulation.

## Slide 19: Application methods
The most common application method for easy-care and durable press finishes is a pad–dry–cure procedure. In this process, the crosslinking reactant, catalyst, softener, and other components are dried on the fabric prior to the crosslinking reaction that takes place during the curing step.

## Slide 22: Compatibility with other finishes
In commercial use, easy-care and durable press finishes are frequently combinedwith other finishes to provide additional properties such as water and oil repellency, flame retardancy, soil release and the like. Often the combination of another finish with the cellulose crosslinking finish will result in a more durable effect from the first finish. Combination with pigment printing is very common because of similar chemistry to cellulose crosslinking agents and binders and the similar application conditions.

## Slide 23: Evaluation methods for formaldehyde
Two useful formaldehyde tests are-
Qualitative test for the presence of formaldehyde in fabrics
Quantitative test for formaldehyde in air

## Slide 24: Qualitative test for the presence of formaldehyde in fabrics
Add a small piece of fabric to 2–3 ml of a solution of 10 mg chromotropic acid per 100 ml of 72 % sulfuric acid. Warm the solution carefully to not more than 100 °C for 1 min. A red to violet colour in the solution indicates the presence of formaldehyde.

## Slide 25: Quantitative test for formaldehyde in air
This is most conveniently done with testing tubes designed for this purpose (Dräger tubes from Drägerwerk AG, Lübeck, Germany, are an example). A colour change to a certain mark after a specified amount of air is drawn through the tube gives the formaldehyde concentration.